Cable Type: Duct cable - non metallic central strength member, stranded loose tubes, filling, wrapping, peripheral strength members, PE sheath

| - not to scale - figure shows: cable with 48 fibres |  | - Central strength element (CSM): FRP - Loose tubes: tubes of thermoplastic material filled with thixotropic compound, containing up to12 fibres - Cable core: 4 loose tubes and 1 filler element are SZ stranded around the central element. The interstices of the cable core are filled with high grade cable filling compound. - Core wrapping: plastic tape - Strain bearing elements: aramide yarns - Sheath: PE, black, nominal radial thickness: 1.5 mm, two rip cords beneath the sheath |
| --- | --- | --- |

Cable Dimensions and main mechanical characteristics

| no. of loose tubes x fibre count per tube | fibre count | cable O.D. | cable weight, approx. | Tensile performance installation / operation | Bending radius installation / operation | CSM O.D. | Loose tubes O.D. |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | [mm] | [kg/km] | [N] | [mm] | [mm] | [mm] |
| 4 x 12 | 48 | 11 | 95 | 1900 / 650 | 220 / 165 | 2.1 | 2.5 |

Mechanical Properties and Delivery Conditions

| standard delivery length | 4 km | transport and storage | -40°C up to +70°C |
| --- | --- | --- | --- |
|  |  | installation | -5°C up to +50°C |

Main Mechanical and Environmental Characteristics

| Test | Test Standard | Specified Value | Acceptance Criteria |
| --- | --- | --- | --- |
| Tensile performance | EN 187000, 501 | kilometric weight * 2 [N] =Tmax kilometric weight * 2 [N] / 3 =T0 |  reversible   0.05 dB/100 m |
| Crush | EN 187000, 504 | 1.5 kN / 100 mm |   0.05 dB |
| Impact | EN 187000, 505 | 10 Nm, r=300 mm, 3 impacts |  reversible |
| Torsion | EN 187000, 508 | 1 m, 180°, 100 N |   0.1 dB/fibre |
| Cable bend | EN 187000, 513 | 15 x cable outer diameter, 5 turns |   0.05 dB |
| Temperature cycling | EN 187000, 601 | -10°C ... +50°C -20°C ... +70°C |   0.05 dB/km   0.1 dB/km |
| Water penetration | EN 187000, 605 | 3m cable, 1m water, 24h | no water leakage |

Identification:

| outer sheath marking |  | identification of loose tubes and fillers within cable core |
| --- | --- | --- |
| The outer cable sheath is marked in white with a sequential length marking in regular intervals of 1 m. Remark: Additional markings upon request. |  | 1. tube: red (marker) 2. tube: green (direction) all other tubes: white filler elements: nature Remark: Other colour codes upon request. |

identification of fibres within loose tube

| fibre no. | colour of fibre | fibre no. | colour of fibre | fibre no. | colour of fibre |
| --- | --- | --- | --- | --- | --- |
| 1 | blue | 5 | grey | 9 | yellow |
| 2 | orange | 6 | white | 10 | violet |
| 3 | green | 7 | red | 11 | pink |
| 4 | brown | 8 | black | 12 | turquoise |